TECHNICAL DATA SHEET

Envirocut SE10

Description

A non-HAP, non-VOC, biodegradable, renewable, fully synthetic ester based product suitable for high performance grinding and machining. The product gives ultimate surface finish and tool-life.

Benefits

| Excellent lubricity | Excellent surface finish |
| --- | --- |
| Excellent EP Performance. | Enhanced Tool-life |
| Cost effective | Very economical in-use |
| Non-HAP | Non hazardous air pollutant. |

Typical Physical Properties

| Appearance | Almost water white |
| --- | --- |
| Specific Gravity | ~0.87 @ 20oC |
| Foaming Tendency | Low |
| Viscosity at 40oC | 10 cSt |
| Flash Point | >210oC |
| Lubricity | Very High |
| Chlorine (elemental) | Nil |
| Sulphur (active) | Nil |
| Usage Concentration | As supplied |

Application Method

Envirocut SE10 is suitable for grinding and machining of all metals.

Envirocut SE10 can be applied in mist and flood applications.