

TECHNICAL DATA SHEET 
Envirocut SE10
Description
A non-HAP, non-VOC, biodegradable, renewable, fully synthetic ester based product suitable for high performance grinding and machining. The product gives ultimate surface finish and tool-life.
Benefits
	· Excellent lubricity
	· Excellent surface finish

	· Excellent EP Performance.
	· Enhanced Tool-life

	· Cost effective
	· Very economical in-use

	· Non-HAP
	· Non hazardous air pollutant.


Typical Physical Properties

	Appearance
	Almost water white

	Specific Gravity
	~0.87 @ 20oC

	Foaming Tendency
	Low

	Viscosity at 40oC
	10 cSt

	Flash Point
	>210oC

	Lubricity
	Very High

	Chlorine (elemental)
	Nil

	Sulphur (active)
	Nil

	Usage Concentration
	As supplied


Application Method
Envirocut SE10 is suitable for grinding and machining of all metals.
Envirocut SE10 can be applied in mist and flood applications.

